## Slide 1: Kinetic Modelling of Fast Catalytic Pyrolysis of biomass
Name: Abhijeet P. Selukar [CA21M001]
Guide: Prof. Himanshu Goyal
Department of Chemical Engineering , IIT Madras

## Slide 3
Fast Pyrolysis
Fast pyrolysis is a technique for thermally breaking down different biomass types in the absence of air or oxygen to produce products based on their nature, such as solid char, liquid oil, and volatile gas.
Fast Catalytic Pyrolysis
Ex-situ : A catalyst is directly combined with the feedstock of a Pyrolysis Reactor.
FCP is an attractive technology that integrates fast pyrolysis of biomass and catalytic upgrading into a single process to produce bio-oil with enhanced quality that could potentially fit into existing infrastructure.
In-situ : The catalyst is directly connected with pyrolysis fumes, resulting in higher quality bio-oil

## Slide 4
Factors affecting pyrolysis process:
Temperature
Retention time
Feedstock composition
Type of catalyst used
Moisture content
Heating rate
Particle size
Fast pyrolysis conditions:
Pyrolysis Temperature= 500 °C
Heating rate is high (1000 °C/s)
Yield: Bio-oil~ 60-70 wt%
Bio-char~ 15-25 wt%
Syn gas ~ 10-15 wt%
Pyrolysis Process
Ref: Advances in Chemical Engineering, Volume 49, Chapter 2 “Mechanistic understanding of thermochemical conversion of polymer and lignocellulosic biomass”

## Slide 5
Iso-thermal method
The iso-thermal method is utilized for kinetic analysis, in which we keep the temperature constant while varying the heating rate to investigate the behavior of kinetic parameters
Iso-conversional method
The iso-conversional method is also used in kinetic analysis to explore the behavior of kinetic parameters by keeping the conversion constant while altering the temperature and heating rate
Kinetic Model
It explains experimental observations, Promotes an understanding of the kinetics of biomass pyrolysis, Simplifies data collection and analysis as well as the numerical implementation

## Slide 6
Distributed Activation Energy Model (DAEM):
𝐥𝐧 𝛃/𝐓^𝟐 =𝐥𝐧⁡((𝐑𝐤_𝟎)/𝐄)+𝟎.𝟔𝟎𝟕𝟓−𝐄/𝐑𝐓
Kissingers-Akhira-Sunose(KAS):
𝐥𝐧 𝛃/𝐓^𝟐 =𝐥𝐧((𝐑𝐤_𝟎)/𝐄𝐆(𝛂) )− 𝐄/𝐑𝐓
Flynn-Wall-Ozawa(FWO):
𝐥𝐧𝛃=𝐥𝐧 (𝟎.𝟎𝟎𝟒𝟖𝐀𝐄)/𝐑𝐆(𝛂) −𝟏.𝟎𝟓𝟐 𝐄/𝐑𝐓
Starink Method:
𝐥𝐧 𝛃/𝐓^(𝟏.𝟗𝟐) = 𝐂_𝐬−𝟏.𝟎𝟎𝟎𝟖 𝐄/𝐑𝐓
Friedman Method:
ln(
ln(𝛃 𝐝𝛂/𝐝𝐭)=𝐥𝐧⁡(𝐤_𝐨 𝐟(𝛂))−𝐄_𝐚/𝐑𝐓
Distributed Activation Energy Model (DAEM):
Kissingers-Akhira-Sunose(KAS):
Flynn-Wall-Ozawa(FWO):
Starink Method:
Friedman Method:
β = Heating Rate
Model-Free Iso-conversional Method:

## Slide 7
Y =
C +
mX
m =
By using this formula we can find out Activation Energy and Pre-Exponential Factor
Distributed Activation Energy Model (DAEM) Equation:
Chart: α = 0.05
| 1.89611307420494E-3 | 1.8734982332155397E-3 | 1.8565371024734901E-3 | 1.8452296819787899E-3
 | 3.0154 | 3.4086 | 3.6696 | 3.87
1/T
I used data from the Research paper Kinetics of Biomass Pyrolysis Using Nickel-Based Functional Materials .In which, they used three types of biomass, straw, sawdust, and cellulose. under three conditions: without catalyst, with Ni-CaO-Si2O4 catalyst and with Ni-Ca2SiO4 catalyst.

## Slide 8
0.05
α
0.9
1/T
50oc/min
40oC/min
30oC/min
20oC/min
Distributed Activation Energy Model

## Slide 9
Chart: Straw
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
KAS:Without catalyst | 141.1322 | 136.7136 | 139.306 | 135.6047 | 134.8248 | 137.9267 | 139.9199 | 133.9503 | 143.9248 | 145.3813 | 138.9646 | 140.1241 | 140.6159 | 142.9051 | 155.2133 | 187.1495 | 231.2139 | 252.7968
KAS:With NiCaOSi2O4 Catalyst | 141.8293 | 136.6895 | 133.1519 | 125.2221 | 132.8879 | 128.1566 | 134.8711 | 127.1852 | 119.7023 | 115.547 | 114.3516 | 88.3881 | 83.3366 | 123.9455 | 117.6575 | 96.0018 | 148.1798 | 161.779
KAS:With NiCa2SiO4 Catalyst | 158.5164 | 144.5805 | 144.378 | 137.9961 | 145.8629 | 137.4022 | 145.6205 | 134.4252 | 137.5952 | 137.5048 | 137.4172 | 143.7138 | 163.5525 | 191.4735 | 210.0109 | 155.1938 | 183.4688 | 191.053
Chart: Straw
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
FWO:Without catalyst | 137.9195 | 138.2822 | 136.26 | 131.1118 | 140.5381 | 147.9859 | 126.7762 | 139.0116 | 169.372 | 127.0566 | 122.3574 | 145.2471 | 146.4744 | 161.3525 | 189.8925 | 220.0651 | 248.1154 | 261.7033
FWO:With NiCaOSi2O4 Catalyst | 139.6982 | 131.9198 | 120.6702 | 131.86 | 133.831 | 135.7202 | 134.6046 | 98.5999 | 99.2043 | 106.4993 | 89.3916 | 58.5326 | 95.9843 | 160.6726 | 110.4105 | 110.0577 | 174.2407 | 181.6787
FWO:With NiCa2SiO4 Catalyst | 150.1296 | 141.4099 | 136.5432 | 120.41 | 142.1149 | 162.967 | 136.5717 | 117.2269 | 144.6624 | 137.4417 | 148.23 | 177.4263 | 209.0069 | 220.3036 | 205.1704 | 146.5045 | 192.1974 | 194.162
Chart: Straw
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
Friedman:Without catalyst | 142.5254 | 138.6691 | 141.3378 | 137.9607 | 137.3325 | 140.3665 | 142.3458 | 136.7326 | 146.2889 | 147.7393 | 141.6933 | 142.858 | 143.3898 | 145.6489 | 157.4684 | 188.09 | 230.5075 | 251.7604
Friedman:With NiCaOSi2O4 Catalyst | 141.8293 | 136.6895 | 133.1519 | 125.2221 | 132.8879 | 128.1566 | 134.8711 | 127.1852 | 119.7023 | 115.547 | 114.3516 | 88.3881 | 83.3366 | 123.9455 | 117.6575 | 96.0018 | 148.1798 | 161.779
Friedman:With NiCa2SiO4 Catalyst | 159.0682 | 146.162 | 146.1596 | 147.5267 | 155.5025 | 147.0314 | 155.4387 | 144.3192 | 147.5673 | 147.5513 | 147.5393 | 153.9252 | 173.8951 | 202.0491 | 221.008 | 166.8315 | 196.0182 | 205.0464
The graph below depicts how activation energy varies :

## Slide 10
Chart: Straw
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
KAS:Without catalyst | 30.3195 | 27.9481 | 27.7897 | 26.5168 | 25.9874 | 26.3466 | 26.5165 | 25.0396 | 26.9058 | 27.0139 | 25.4852 | 25.5361 | 25.4617 | 25.6765 | 27.7393 | 33.0399 | 39.2828 | 40.0914
KAS:With NiCaOSi2O4 Catalyst | 30.1984 | 27.697 | 26.3324 | 24.177 | 25.4721 | 24.1741 | 25.3312 | 23.4745 | 21.6322 | 20.4814 | 19.8783 | 14.1264 | 12.5595 | 19.3825 | 16.3434 | 10.9801 | 17.4601 | 18.6646
KAS:With NiCa2SiO4 Catalyst | 34.3529 | 29.6821 | 28.9212 | 27.0414 | 28.099 | 26.7299 | 27.7439 | 25.1621 | 25.5822 | 25.3436 | 25.1057 | 26.1016 | 29.6926 | 34.375 | 36.3805 | 24.3776 | 26.9924 | 24.8884
Chart: Straw
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
FWO:Without catalyst | 30.7138 | 28.4821 | 28.3323 | 27.1419 | 26.6477 | 26.9809 | 27.1406 | 25.7607 | 27.5032 | 27.6053 | 26.1747 | 26.2222 | 26.1538 | 26.3538 | 28.2802 | 33.2684 | 39.1982 | 39.9622
FWO:With NiCaOSi2O4 Catalyst | 30.6013 | 28.2444 | 26.9703 | 24.9632 | 26.1649 | 24.9575 | 26.0326 | 24.3066 | 22.5995 | 21.5381 | 20.9835 | 15.7678 | 14.3697 | 20.5198 | 17.7402 | 12.948 | 18.7459 | 19.8407
FWO:With NiCa2SiO4 Catalyst | 34.5255 | 30.111 | 29.3946 | 27.5821 | 28.7856 | 27.3991 | 28.2381 | 25.8259 | 26.2162 | 25.9932 | 25.771 | 26.6973 | 30.0626 | 34.4817 | 36.3833 | 25.0774 | 27.5145 | 25.5428
Chart: Straw
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
Friedman:Without catalyst | 39.6489 | 38.7786 | 38.0969 | 36.8352 | 38.7343 | 40.1944 | 35.6233 | 38.0683 | 44.1706 | 35.3131 | 34.1999 | 38.7129 | 38.6459 | 41.0293 | 45.7299 | 49.7963 | 52.2794 | 51.5679
Friedman:With NiCaOSi2O4 Catalyst | 36.2891 | 33.7016 | 31.0611 | 33.3898 | 33.6613 | 33.8916 | 33.4881 | 25.6376 | 25.4174 | 26.5079 | 22.3577 | 15.2929 | 21.9864 | 32.6036 | 21.263 | 19.5481 | 28.2025 | 28.8222
Friedman:With NiCa2SiO4 Catalyst | 42.4529 | 39.481 | 38.1865 | 34.5429 | 39.181 | 44.0316 | 37.6464 | 33.4345 | 38.9374 | 37.2645 | 39.1564 | 44.5218 | 49.9281 | 50.6143 | 45.6777 | 32.7987 | 38.1308 | 35.0131
The graph below depicts how Pre-exponential Factor varies :

## Slide 11: Types of model
Nucleation-based model(P)
Geometrical contraction-based model(A,F)
Diffusion model(D)
Order-based model (R)
Master plot: It is a graphical method used to study the kinetic behavior of a substance, by plotting the variation of some characteristic quantity.

## Slide 12
Chart: Straw
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
R2 | 0.0475 | 0.09 | 0.1275 | 0.16 | 0.1875 | 0.21 | 0.2275 | 0.24 | 0.2475 | 0.25 | 0.2475 | 0.24 | 0.2275 | 0.21 | 0.1875 | 0.16 | 0.1275 | 0.09
R3 | 0.046313 | 0.0855 | 0.11794 | 0.144 | 0.16406 | 0.1785 | 0.18769 | 0.192 | 0.19181 | 0.1875 | 0.17944 | 0.168 | 0.15356 | 0.1365 | 0.11719 | 0.096 | 0.073313 | 0.0495
R4 | 0.045165 | 0.0813 | 0.10933 | 0.13013 | 0.14453 | 0.1533 | 0.15716 | 0.1568 | 0.15283 | 0.14583 | 0.13633 | 0.1248 | 0.11166 | 0.0973 | 0.082031 | 0.066133 | 0.049831 | 0.0333
Exp | 0.034129 | 0.052035 | 0.085858 | 0.12269 | 0.14747 | 0.17219 | 0.20334 | 0.22408 | 0.24189 | 0.24629 | 0.23978 | 0.26595 | 0.24259 | 0.16222 | 0.083888 | 0.035384 | 0.019387 | 0.017378
F5 | 0.475 | 0.45 | 0.425 | 0.4 | 0.375 | 0.35 | 0.325 | 0.3 | 0.275 | 0.25 | 0.225 | 0.2 | 0.175 | 0.15 | 0.125 | 0.1 | 0.075 | 0.05
D1 | 0.025 | 0.05 | 0.075 | 0.1 | 0.125 | 0.15 | 0.175 | 0.2 | 0.225 | 0.25 | 0.275 | 0.3 | 0.325 | 0.35 | 0.375 | 0.4 | 0.425 | 0.45
D2 | 0.024786 | 0.049122 | 0.072969 | 0.096284 | 0.11901 | 0.1411 | 0.16247 | 0.18305 | 0.20271 | 0.22135 | 0.23878 | 0.25481 | 0.26915 | 0.28141 | 0.29101 | 0.29707 | 0.29805 | 0.29087
Z(α)-2 | 0.037338 | 0.05689 | 0.096902 | 0.12484 | 0.14689 | 0.18234 | 0.18169 | 0.18425 | 0.16591 | 0.14904 | 0.11331 | 0.094396 | 0.072878 | 0.033118 | 0.024505 | 0.03596 | 0.050333 | 0.066823
Z(α)-3 | 0.030808 | 0.051431 | 0.084089 | 0.12601 | 0.14653 | 0.16922 | 0.18955 | 0.21368 | 0.20888 | 0.22115 | 0.19096 | 0.13734 | 0.084899 | 0.043585 | 0.026381 | 0.026101 | 0.017298 | 0.016044
Master plot for Straw with three Conditions:
….…: Without Catalyst ….… : With Ni-CaOSi2O4 Catalyst ….…: With Ni-Ca2SiO4 Catalyst

## Slide 13
Chart: Sawdust
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
R2 | 0.0475 | 0.09 | 0.1275 | 0.16 | 0.1875 | 0.21 | 0.2275 | 0.24 | 0.2475 | 0.25 | 0.2475 | 0.24 | 0.2275 | 0.21 | 0.1875 | 0.16 | 0.1275 | 0.09
R3 | 0.046313 | 0.0855 | 0.11794 | 0.144 | 0.16406 | 0.1785 | 0.18769 | 0.192 | 0.19181 | 0.1875 | 0.17944 | 0.168 | 0.15356 | 0.1365 | 0.11719 | 0.096 | 0.073313 | 0.0495
R4 | 0.045165 | 0.0813 | 0.10933 | 0.13013 | 0.14453 | 0.1533 | 0.15716 | 0.1568 | 0.15283 | 0.14583 | 0.13633 | 0.1248 | 0.11166 | 0.0973 | 0.082031 | 0.066133 | 0.049831 | 0.0333
R6 | 0.048109 | 0.09237 | 0.13268 | 0.16892 | 0.20096 | 0.22868 | 0.25191 | 0.27048 | 0.28422 | 0.29289 | 0.29626 | 0.29404 | 0.28587 | 0.27137 | 0.25 | 0.22111 | 0.18381 | 0.13675
R5 | 0.044055 | 0.077377 | 0.10157 | 0.11808 | 0.12817 | 0.13298 | 0.13349 | 0.13056 | 0.12492 | 0.11719 | 0.10789 | 0.09744 | 0.086187 | 0.074393 | 0.062256 | 0.04992 | 0.037481 | 0.024997
Exp | 0.041963 | 0.059774 | 0.093856 | 0.11287 | 0.13791 | 0.14746 | 0.16932 | 0.17932 | 0.18686 | 0.20568 | 0.22603 | 0.27511 | 0.27445 | 0.25129 | 0.23972 | 0.21292 | 0.10413 | 0.028048
D1 | 0.025 | 0.05 | 0.075 | 0.1 | 0.125 | 0.15 | 0.175 | 0.2 | 0.225 | 0.25 | 0.275 | 0.3 | 0.325 | 0.35 | 0.375 | 0.4 | 0.425 | 0.45
D2 | 0.024786 | 0.049122 | 0.072969 | 0.096284 | 0.11901 | 0.1411 | 0.16247 | 0.18305 | 0.20271 | 0.22135 | 0.23878 | 0.25481 | 0.26915 | 0.28141 | 0.29101 | 0.29707 | 0.29805 | 0.29087
F4 | 0.95 | 0.9 | 0.85 | 0.8 | 0.75 | 0.7 | 0.65 | 0.6 | 0.55 | 0.5 | 0.45 | 0.4 | 0.35 | 0.3 | 0.25 | 0.2 | 0.15 | 0.1
P2 | 0.033333 | 0.066667 | 0.1 | 0.13333 | 0.16667 | 0.2 | 0.23333 | 0.26667 | 0.3 | 0.33333 | 0.36667 | 0.4 | 0.43333 | 0.46667 | 0.5 | 0.53333 | 0.56667 | 0.6
Z(α)-2 | 0.047122 | 0.068701 | 0.0998 | 0.12045 | 0.13839 | 0.15937 | 0.17777 | 0.21568 | 0.22655 | 0.23365 | 0.25427 | 0.25044 | 0.20617 | 0.15209 | 0.079241 | 0.035545 | 0.041775 | 0.035018
Z(α)-3 | 0.045709 | 0.063672 | 0.090368 | 0.11648 | 0.14113 | 0.15885 | 0.17389 | 0.188 | 0.20202 | 0.22124 | 0.23804 | 0.26597 | 0.27105 | 0.23817 | 0.24842 | 0.15185 | 0.033546 | 0.024746
Master plot for Sawdust with three Conditions:
….…: Without Catalyst ….… : With Ni-CaOSi2O4 Catalyst ….…: With Ni-Ca2SiO4 Catalyst

## Slide 14
Chart: Cellulose
| 0.05 | 0.1 | 0.15 | 0.2 | 0.25 | 0.3 | 0.35 | 0.4 | 0.45 | 0.5 | 0.55000000000000004 | 0.6 | 0.65 | 0.7 | 0.75 | 0.8 | 0.85 | 0.9
A1 | 0.073093 | 0.14224 | 0.20721 | 0.26777 | 0.32364 | 0.37451 | 0.42001 | 0.45974 | 0.49322 | 0.51986 | 0.53899 | 0.54977 | 0.55116 | 0.54179 | 0.51986 | 0.48283 | 0.42685 | 0.34539
A2 | 0.097457 | 0.18965 | 0.27628 | 0.35703 | 0.43152 | 0.49934 | 0.56002 | 0.61299 | 0.65762 | 0.69315 | 0.71866 | 0.73303 | 0.73488 | 0.72238 | 0.69315 | 0.64378 | 0.56914 | 0.46052
Exp | 0.10683 | 0.14789 | 0.21835 | 0.30012 | 0.3776 | 0.40912 | 0.49492 | 0.51048 | 0.4655 | 0.49708 | 0.55863 | 0.67958 | 0.64124 | 0.49623 | 0.4503 | 0.3897 | 0.31907 | 0.30241
D1 | 0.025 | 0.05 | 0.075 | 0.1 | 0.125 | 0.15 | 0.175 | 0.2 | 0.225 | 0.25 | 0.275 | 0.3 | 0.325 | 0.35 | 0.375 | 0.4 | 0.425 | 0.45
D2 | 0.024786 | 0.049122 | 0.072969 | 0.096284 | 0.11901 | 0.1411 | 0.16247 | 0.18305 | 0.20271 | 0.22135 | 0.23878 | 0.25481 | 0.26915 | 0.28141 | 0.29101 | 0.29707 | 0.29805 | 0.29087
F2 | 0.049359 | 0.097367 | 0.14391 | 0.18885 | 0.23205 | 0.27332 | 0.31245 | 0.34919 | 0.38324 | 0.41421 | 0.44164 | 0.46491 | 0.48322 | 0.49545 | 0.5 | 0.49443 | 0.4746 | 0.43246
F4 | 0.95 | 0.9 | 0.85 | 0.8 | 0.75 | 0.7 | 0.65 | 0.6 | 0.55 | 0.5 | 0.45 | 0.4 | 0.35 | 0.3 | 0.25 | 0.2 | 0.15 | 0.1
F5 | 0.475 | 0.45 | 0.425 | 0.4 | 0.375 | 0.35 | 0.325 | 0.3 | 0.275 | 0.25 | 0.225 | 0.2 | 0.175 | 0.15 | 0.125 | 0.1 | 0.075 | 0.05
Z(α) | 0.10867 | 0.14299 | 0.22108 | 0.28778 | 0.30462 | 0.32188 | 0.37166 | 0.50603 | 0.47633 | 0.42954 | 0.46756 | 0.4025 | 0.33214 | 0.30349 | 0.23516 | 0.15407 | 0.067873 | 0.041636
Z(α) | 0.098409 | 0.13818 | 0.21113 | 0.25746 | 0.31927 | 0.38223 | 0.40336 | 0.48703 | 0.50735 | 0.47154 | 0.51431 | 0.55235 | 0.5561 | 0.49121 | 0.42933 | 0.37386 | 0.25415 | 0.18834
R2 | 0.0475 | 0.09 | 0.1275 | 0.16 | 0.1875 | 0.21 | 0.2275 | 0.24 | 0.2475 | 0.25 | 0.2475 | 0.24 | 0.2275 | 0.21 | 0.1875 | 0.16 | 0.1275 | 0.09
R3 | 0.046313 | 0.0855 | 0.11794 | 0.144 | 0.16406 | 0.1785 | 0.18769 | 0.192 | 0.19181 | 0.1875 | 0.17944 | 0.168 | 0.15356 | 0.1365 | 0.11719 | 0.096 | 0.073313 | 0.0495
Master plot for Cellulose with three Conditions:
….…: Without Catalyst ….… : With Ni-CaOSi2O4 Catalyst ….…: With Ni-Ca2SiO4 Catalyst

## Slide 15: Conclusion
The functional materials, Ni-CaOCa2SiO4 and Ni-Ca2SiO4, showed an obvious catalytic effect for the three types of biomass samples tested
The correlation R2 of all fitting lines in all cases was above 0.9, which indicated that FWO method, KAS method, Friedman method and DAEM were suitable for modelling the kinetics of biomass catalytic pyrolysis whereas FWO method, KAS method, DAEM showed more accuracy as compare Friedman method.
For the three types of biomasses tested, the functional material, NiCaOCa2SiO4, showed the greatest catalytic effect on pyrolysis due to the evident decrease in activation energy. For sawdust, the functional material, Ni-Ca2SiO4 Catalyst showed Greater catalytic effect as compared to , NiCaOCa2SiO4 Catalyst
significant impact of catalysts on the reaction mechanisms. The use of NiCaOSi2O4 catalyst altered the reaction pathway, with involvement of nucleation, diffusion control, and multiple reaction mechanisms. The presence of catalysts provided better control over the conversion process and facilitated the production of targeted biofuels..

## Slide 16: Reference
Liu, C., Wang, H., Karim, A. M., Sun, J., & Wang, Y. (2014). Catalytic fast pyrolysis of lignocellulosic biomass. Chemical Society Reviews, 43(22), 7594-7623.
Yang, Hang, et al. "Kinetics of catalytic biomass pyrolysis using Ni-based functional materials." Fuel Processing Technology 195 (2019): 106145.
Performance-screening of metal-impregnated industrial HZSM-5/γ-Al2O3 extrudates for deoxygenation and hydrodeoxygenation of fast pyrolysis vapors - ScienceDirect
Thank You